## Slide 1: Low-Pressure Electrolytic Ammonia (LPEA) Production DE-EE0008324 University of North Dakota (UND) Energy & Environmental Research Center (EERC) North Dakota State University Nel Hydrogen (NEL)/Proton OnSite 15 June 2018 – 14 June 2021
Ted Aulich, EERC
U.S. DOE Advanced Manufacturing Office Virtual Program Review
June 2-3, 2020
This presentation does not contain any proprietary, confidential, or otherwise restricted information.

## Slide 2: Overview
Timeline:
Project Start Date: 06/15/2018
Budget Period End Date: 06/14/2021
Project End Date: 06/14/2021
Budget | DOE Share | Cost Share | Total | Cost Share %
Overall Budget | $ 2,497,983 | $ 666,027 | $3,164,010 | 21.1%
Approved Budget (BP 1&2) | $ 2,497,983 | $ 666,027 | $3,164,010 | 21.1%
Costs as of 3/31/20 | $ 1,329,033 | $ 436,860 | $1,765,893 | 24.7%
Project Budget and Costs:
Barriers and Challenges:
Develop gas-tight, durable, high-proton-conductivity (10-2 siemens/cm (S/cm) proton exchange membrane capable of sustained operation at 300°–325°C in acidic environment.
Integrate membrane with appropriate anode and cathode catalysts in a membrane–electrode assembly (MEA) to produce ammonia at ambient pressure
Project Team and Roles:
University of North Dakota/EERC (Lead):
Direct membrane and MEA fabrication efforts
Evaluate membrane and MEA performance, durability
Identify best available cathode catalyst(s) for nitrogen reduction (ammonia synthesis)
Assess LPEA process techno-economic viability
North Dakota State University (NDSU) – Develop and optimize membrane fabrication technique
Nel Hydrogen – Develop and optimize MEA fabrication technique
AMO MYPP Connection:
Process Intensification
Project Title:
Low-Pressure Electrolytic Ammonia Production
Example 1

## Slide 3
Current Haber Bosch- (HB-) based ammonia production processes need high pressure (1100–3000 psi) to achieve economically viable ammonia yields (15%–18% based on single-pass hydrogen conversion).
High pressure translates to:
  High capital cost (large compressor and system-wide high-pressure compatibility).
  High energy consumption/operating cost (need to compress both new and recycled reactants).
Project Goal – Eliminate need for high pressure by optimizing electricity-driven process that enables control of ammonia formation reaction on catalyst surface; achieve 16% input energy reduction vs state-of-the-art (2018) HB-based processes—8.5 to 7.4 MWh/ton ammonia.
  Keys to achieving goal:
    Optimize high-temperature (300–325°C) high-proton-conductivity gas-impermeable polymer–inorganic composite (PIC) proton exchange membrane (primary project challenge)
    Identify (not develop) best available cathode catalyst (for N2 reduction/NH3 synthesis)
Project Objectives

## Slide 4: Technical Innovation
In addition to high-pressure to push ammonia synthesis reaction forward, HB process needs temperature between about 350-450°C, because:
  High temp necessary to crack highly stable N2 triple bond.
  Above 450°C, equilibrium pushes reaction backwards.
However, most HB-alternative electrolytic ammonia technology development efforts are focused on low-temp (ambient—150°C) or high-temp (≥500°C) to enable use of low-temp polymer membranes or high-temp SOFC electrolytes, respectively.
By offering high proton conductivity (≥10-2 siemens/cm) and low H2 permeability at 300°–325°C, PIC proton exchange membrane (project goal) will enable operation at near-optimum temp for ammonia formation at high rate needed for commercial viability.
PIC membrane comprises low-cost (no precious metals) inorganic proton conductor (IPC) particles strategically composited in affordable, commercially available high-temperature polymer matrix.

## Slide 5: Technical Approach
Optimize methods for inorganic proton conductor (IPC) synthesis and particle size reduction (≤5 microns is current target).
  Performer – EERC
Optimize “solution/film-casting” method for fabrication of 100-micron-thick PIC membrane comprising ≥80 wt% IPC; evaluate and optimize membrane based on proton conductivity, H2 permeability, and durability at 300°–325°C.
  Performers – NDSU (fabrication); EERC (evaluation); Both (optimization)
Screen candidate cathode catalysts based on N2 electroreduction faradaic efficiency and current density achievable in room-temp H-cell aqueous electrolyte system.
  Performer – EERC
Using PIC membrane, best-performing cathode catalyst, commercial PEM electrolyzer anode catalyst, fabricate MEAs; evaluate at ≥300°C, optimize based on ammonia synthesis faradaic efficiency and current density.
  Performers – Nel (fabrication); EERC (evaluation); Both (optimization)

## Slide 6: Technical Approach-2
Major project risks are inability to achieve and sustain PIC membrane performance targets (at minimum 300°C operating temp) of:
  Proton conductivity – 10-2 siemens/cm
  H2 permeability – <2% of H2 fed to anode chamber
Project team attributes relevant to addressing these risks are
NDSU polymer science and engineering expertise utilized in tailoring membrane solution casting method for “colloidal suspension” casting to accommodate incorporation and distribution of inorganic proton conductor (IPC) particles.
EERC materials science experience utilized in identifying and developing synthesis method for IPC and cathode catalyst.
Nel commercial expertise in MEA manufacturing.
If risk(s) realized, mitigation and/or work-around strategies will involve:
Transition from membrane to thin slab able to hold more IPC and/or decrease H2 permeability; trade-off is less flexibility, which may translate to more difficulty in achieving gas-tight seal.
Explore options for “solvent-less” membrane fabrication from dry mix of polymer and IPC particles using high-pressure heat pressing at polymer glass transition temperature to eliminate membrane void spaces.

## Slide 7: Results and Accomplishments
Produced PIC membrane with measured (inferred via alternating current impedance spectroscopy) 300°C proton conductivity (PC) of 0.5*10-2 siemens/cm (S/cm).
Identified low-cost metal cathode catalyst with 11% faradaic efficiency for nitrogen reduction at room temperature.
Produced initial MEA using partially optimized PIC membrane, low-cost metal cathode catalyst, and platinum anode catalyst. At 300°C, MEA exhibited stable PC (actual, not inferred) of 0.9*10-2 siemens/cm (S/cm), 90% of project goal (1*10-2 S/cm).

## Slide 8: Results and Accomplishments-2
Work needed between now and 14 June 2021 project end date:
  Optimize PIC membrane, cathode catalyst, and MEA to achieve—in unit cell/MEA tests—ammonia synthesis at milestone goals of:
  Current density ≥0.25 amps/cm2
  Current efficiency ≥65%
  Production energy efficiency ≥65%
  ≤0.3% performance degradation/1000 hours
Build multi-cell/MEA stack capable of ≥100-grams/day ammonia production; conduct long-term testing to acquire data for techno-economic assessment, with project goal of demonstrating ammonia production at total energy consumption of 7.4 MW/ton

## Slide 9: Transition (beyond DOE assistance)
TRL of 4–5 anticipated at project end
Use techno-economic analysis results to secure arrangements with utility or ammonia production facility for pilot-scale demo
Use demo results to negotiate nonexclusive licenses with:
  Fuel cell/electrolyzer and/or MEA manufacturer
  Engineering/design firms that service ammonia, chemical, power industries
Use demo results to market LPEA as:
  Option for integration into existing ammonia supply chain to replace portions of and/or supplement current HB infrastructure
  Means for monetizing renewable energy and/or utilizing low-cost off-peak power