## Slide 1
Materials for Harsh
Service Conditions:
High Temperature Corrosion
Brian Gleeson
DOE-EERE Workshop
Pittsburgh, PA
November 19 & 20, 2015

## Slide 2
Harsh Environments
at High Temperatures
SO4
2-
Courtesy: Michael Schütze (DECHEMA)

## Slide 3: Common Forms of High-Temperature Degradation
Oxidation (O2, H2O, CO2 )
Sulfidation (S2, H2S)
Oxidation/Sulfidation (SO2, SO3)
Carburization (CO, CH4)
Nitridation (N2, NH3)
Chloridation (Cl2, HCl)
Hot Corrosion (Na2SO4)
Ash Deposit (fly ash)
Many operating environments are multi-oxidant.
Even so, resistance to degradation often requires the
formation of a protective oxide.
Deposit-induced attack
volatilization contribution to attack

## Slide 4: High-Temperature Materials
Important focus: Surface Degradation of Materials for Exposure to Harsh Environments
Assessment, development and modification of materials and surfaces for extended performance in many high-temperature applications, including advanced energy-generating systems.
Al2O3
Single Crystal Ni-base Superalloy

## Slide 5: Isothermal Oxidation Kinetics at 1150˚C (2102˚F) in Air Single Doped : Hf vs. Y
-0.05Hf
-0.05Y
Ni-20Al-5Cr
Base composition (at.%): Ni-20Al-5Cr
Al2O3 scale
Al2O3 scale

## Slide 6
Effect of Minor Element Contents Wrought 800 alloys from two different producers
Alloys | C | Mn | Si | Cr | Ni | Fe | Ti | Al | Cu
A800 | 0.02 | 0.78 | 0.13 | 20.05 | 33.64 | 44.46 | 0.41 | 0.30 | 0.21
B800 | 0.06 | 0.70 | 0.38 | 20.50 | 30.30 | 47.15 | 0.32 | 0.25 | 0.07
Measured compositions in wt.%
0
20
40
60
80
100
120
-100
-80
-60
-40
-20
0
B800
A800
Weight Change(mg/cm2 )
Oxidation cycles
1000ºC, 1-day cycles
Oxidation behavior is often significantly influenced by minor alloying additions

## Slide 7
No deposit
STEM images
SiO2-Al2O3-CaO-Na2SO4 deposit
500 nm
500 nm
deposit
Al, Cr oxide
Al2O3-Scale Formation on an NiCoCrAlY System
Ni-30Co-30Cr-12Al-0.1Y in CO2-20H2O-1.6O2 at 1100 °C in air
Al2O3
After 20 minutes
After 50 hours

## Slide 8
NiO+Int.Oxi.
Al2O3
NAl*
#1
#2
#3
#4
Cr2O3
A Steam-Containing Environment can be Harsh
#2
#3
#4
#1
Wet (30% steam)
Al2O3
NAl*
#1
#2
#3
#4
Wet
Cr2O3
NiO+Int.Oxi.
#2
#3
#4
#1
Dry
Giggins and Pettit* established the following oxidation map for rolled Ni-Cr-Al alloys in 0.1atm O2 at 1000oC.
8
*Giggins and Pettit, J. Electrochem. Soc.,118 (1971) 1782

## Slide 9
316 Stainless Steel (18.6 wt % Cr) 650º C for 1500 h
300 bar 1 bar
Effect of Steam Pressure
50 µm
50 µm
Extensive attack
Minimal attack
Courtesy: Alina Aguero (INTA, Spain)

## Slide 10
Oxidation of Fe-15Cr in O2 vs. CO2 at 900C
From F. Pettit and G. Meier, Univ. Pitt.
Predictability of the bi-oxidant CO2 result currently does not exist.

## Slide 11: High-Temperature Degradation Gaps/Opportunities to be Discussed
Environments and materials are typically much more complex than what is treated experimentally or theoretically.
multi-component materials comprised of more than one phase
Multi-oxidant environments
There is a continual push for higher temperatures.
There is often a superpositioning of degradation modes (e.g., mechanical fatigue together with oxidation) in practical applications.
Significant opportunities exist to exploit advanced computation, simulation and characterization techniques.
There is a significant need for improved testing procedures and capabilities.
There is a strong push to develop new materials at a faster pace with reduced risk.

## Slide 12: Cyclic Oxidation of Ni-20Al-(5-10)Cr-0.05Hf Alloys at 1150C
Predicted alloy phase
equilibria

## Slide 13: 700oC Hot Corrosion-Volume Fraction of β-NiAl, Vf(β) Na2SO4 Deposit, O2-1000ppmSO2, 5×20h cycles
Ni-18Co-26Al-20Cr-0.1Y
Vf (β)=77%
Ni-18Co-18Al-28Cr-0.1Y
Vf (β)=46%
Ni-20Co-12Al-35Cr-0.1Y
Vf (β)=18%
Poor resistance
∆m = 33 mg/cm2
Good resistance
∆m = 4.85 mg/cm2
(Ni,Co)O
Excellent resistance
∆m = 0.19 mg/cm2
Na2SO4 Salt
Na2SO4 Salt
Corrosion product

## Slide 14
Multiple crack origins at coating surface
g’-depleted zone around crack
Oxide-filled crack
crack branching
Oxidation-Fatigue Damage
Courtesy: Ram Darolia (GE)
Example of concurrent degradation modes

## Slide 15: Priority Future Research Directions Include:
Understanding the surface-reaction behavior of multiphase materials exposed to multi-component reactive gases …. with and without the inclusion of deposits
Accounting for concurrent degradation processes (e.g., surface reactions during mechanical loading).
Developing lab-scale testing procedures that accurately represent what is found in practice.
Addressing these priorities can be facilitated by the use of advanced computation and characterization techniques.
Probing different temporal and spatial scales

## Slide 16
Thank you for your attention

## Slide 18
Forming and Sustaining a Protective Scale
Spallation Behavior Scale Adherence Diffusion Behavior in Alloy
Scale
Alloy
- Composition
- Strength
- CTE, E
- Microstructure
A systems approach is required:
Oxidant Supply
Deposit
There are important fundamental aspects to each component of this system.

## Slide 19: Cyclic Oxidation Kinetics at 1150˚C (2102˚F) in Air Single doped with Hf or Y vs. Co-doped with Hf+Y
0.1Hf-0.05Y
-0.05Hf
Base composition (at.%): Ni-20Al-5Cr

## Slide 20: Factors Affecting Oxidation
It is well established that oxide formation on an alloy surface is a function of numerous variables, including:
structure and crystallographic orientation of the surface
material microstructure (phases, defects, etc)
the principal oxidizing species (i.e., O2, CO2, or H2O) and its partial pressure
alloy composition and, in particular, surface composition
oxide stabilities and competitive nucleation/growth processes
Compounding factors such as an imposed stress, thermal cycling, erosion, etc.
Many of these factors are well established, but are poorly understood
from a fundamental standpoint

## Slide 21: Fundamental Questions Related to Surface Reactions Include:
To what extent does oxidation behavior change when complexities like loading (cyclic or static), deposits and/or or additional oxidants are imposed?
Can steady-state scaling kinetics be influenced in a controllable manner by the product formed in the very early stages of exposure?
Can reaction behavior be effectively modeled for multi-component systems exposed to multi-oxidant conditions?

## Slide 22: Isothermal oxidation behavior of Ni-20Al-5Cr-based -Ni+-Ni3Al alloys single vs. co-doping
-0.05Hf
-0.05Y
-0.05Hf-0.05Y
-0.1Hf-0.05Y
The oxidation rates of co-doped alloys are between those of Hf- and Y-doped alloys