## Slide 1
Advanced Manufacturing Office
Materials in a High Temperature Service Environment
Professor John H. Perepezko
University of Wisconsin-Madison
Department of Materials Science and Engineering
1509 University Ave.
Madison, WI 53706
Materials for Harsh Service Conditions Workshop
November 19-20, 2015, Westin Convention Center Hotel
Pittsburgh, PA

## Slide 2
Challenges for Materials Performance in a Harsh High Temperature
Service Environment
Temperature range
  1) 1200-1850 F (648-1010 C) – Current/Near Term
  2) >1850 F—Longer Term
Environmental/Service Degradation
  Oxidation – Isothermal; Thermal Cycling
  Hot Corrosion (fuel impurities)
  CMAS (Sand, Ash)
  Steam
  Creep Rupture/Fatigue
  Wear/ Erosion
  Phase Stability – Long Term
  Microstructural Stability- Long Term
  Long Term life prediction

## Slide 3
Applications
  Transportation
  Fossil Fuel
  Nuclear
  Solarthermal
  Geothermal
Manufacturing
  Scale up – Lab ScaleCommercial
  Low Cost
  Low Density
  Performance Diagnostics-In-Situ Sensors
  Sustainability
    Environmental
    Recycle
    Materials Availability

## Slide 5
The Hotter The Better

## Slide 7
Materials Options

## Slide 8
Solarthermal Reactors require high temperatures for power generation and chemical
reactions. Several key components require new materials to achieve potential.

## Slide 9
1-TBC/EBC
2-Oxidation Resistant
3-Compatibility (Bond Coat)
4-Reservoir/Diffusion Barrier
Substrate
Functional Coating Design – Environmental Resistance
Layers/Substrate mechanical compatibility
Layers/Substrate thermodynamic compatibility
At ultrahigh temperature silica is favored
over alumina.

## Slide 10
Progress-Mo-Si-B Coated Pure Molybdenum
Oxidized in Air at 1700oC/3092oF
1700oC / 2 hrs
1700oC / 12 hrs
1700oC / 25 hrs
Mass Change:
+ 1.7 mg/cm2 (1700oC /25hrs)

## Slide 11
The Path Forward - Materials Challenges/Strategies
Incremental (1200-1850F)
  Ultrahigh Strength Steels (Alumina Former)
    ODS—Manufacturing Scaleup
    Austenitic with intermetallics—Phase Stability
Functional Coatings
  Semi-Empirical to Guided Design- Thermodynamic (Calphad); Mechanical
  Application Methods- Commercial Scale
  Amorphous/Nanocrystalline Wear/Corrosion
  Environmental Barrier Coatings, EBC (Silica)
Longer Term – Ultrahigh Temperature (>1850F)- High Payoff
  Refractory Metal (Mo, Nb)Alloys (Mechanical, Silica Former)
  Ceramic Composites – SiC/SiC (EBC, Processing)
  Advanced Coating Capability