## Slide 1: Degradation Mechanisms and Development of Protective Coatings for TES and HTF Containment Materials
National Renewable Energy Laboratory (NREL)
SunShot Lab Proposal Development Process (LPDP)
Dr. Judith Gomez (Vidal), NREL - Materials Engineer IV
Profs. M. Anderson and K. Sridharan from University of Wisconsin

## Slide 2: Project Objective
Acquire understanding of fundamental degradation mechanisms of materials in molten salts (MS) and supercritical CO2 (sCO2) to extend their lifetime to 30 years at the SunShot relevant temperatures of 600 to 800°C using corrosion mitigation approaches.
Project Duration:
    3 years and 5 months
Project Budget:
    $2,610,145

## Slide 3: Corrosion in Molten Salts (MS)
Eutectics MS evaluated: (Na,Li)Cl, (Zn,K)Cl, (Na,K)Cl, (Mg,K)Cl, (Na,K)CO3, and (Na,K,Li)CO3 in N2, Ar, CO2, or ZA atmospheres.
Probabilistic cost analyses probed that there is a clear cost benefit for using protective coatings to tanks and other CSP components.
Conventional long-term weight-change and electrochemical techniques were employed for MS.

## Slide 4: Electrochemical Techniques
The corrosion rate (CR), is calculated using the Stern-Geary equation through Faraday’s Law:
(1)
where K is a constant equal to 3272 [mm/(A·cm·year)], EW is the equivalent weight of the alloy (g/mole-e), and ρ is the alloy density (g/cm3).
Potentiodynamic polarization sweep (PPS)
Nyquist plots (schematic impedance spectrum) with equivalent circuit models for (a) Protective scale, and (b) Localized corrosion
Electrochemical impedance spectroscopy (EIS)
(a)
(b)
EIS does not disturb the equilibrium of the sample
Using the Tafel slopes (anodic: βa and cathodic: βc) from PPS curves, Icorr is determined:
(2)
βa
βc

## Slide 5: Corrosion in Molten Carbonates
Pre-oxidized Ni-Base Coatings
There is no indication of relatively coarse pitting or corrosion attack.
The spheroidal porosity (not connected) did not allow the penetration/permeation of the molten salt.
EDS [wt.%] | Phase |  | 
 | 2a | 2b | 2c
C | 0.9 | 0.9 | 4.4
O | 39.0 | 2.3 | 22.2
Al | 44.2 | 9.8 | 17.8
Cr | 1.4 | 20.0 | 12.0
Co | 1.9 | 23.7 | 13.3
Ni | 2.7 | 46.4 | 21.9
Y | 9.9 | - | -
K | - | - | 1.1
Na | - | - | 6.3
a) SE-SEM, (b) BSE-SEM of APS-NiCoCrAlHfSiY (CR = 34 µm/year) pre-oxidized (air, 900°C, 24 h, 0.5°C /min) and exposed to molten carbonate at 700°C
(a)
(b)
Corrosion rates (CR) of bare and coated alloys in eutectic Na2CO3 – K2CO3 – Li2CO3 at 600º, 650º and 700ºC in N2(g) and CO2(g) atmospheres
34 µm/year (APS-NiCoCrAlHfSiY)
46 µm/year (HVOF-CoNiCrAlY)
Best two coatings exposed to MS in bone-dry CO2 at 700°C.

## Slide 6: Corrosion in Molten Chlorides
Castable Cements
Silica-based castable cements with BN films, to block the porosity, were capable of protecting containment metallic alloys from the attack of molten chlorides at high temperatures (650°C). The cements were not chemically stable in KNa-CO3 at 750°C and KNaLi-CO3 at 600°C.

## Slide 7: Pre-oxidized Ni-Base Coatings
The multiphase dark "wavy" or "swirled" constituent in a light contrasted matrix is consistent with those observed for thermally sprayed coatings. The swirly dark phase is higher in Al and O, presumably alumina. The surface is comprised by a mixture of Al-rich, Cr-rich and possibly Y-rich oxide phases.
Original flat surface is remaining after salt exposure characteristic of low corrosion obtained.
At 700°C the corrosion of 310SS in carbonates (2.456 mm/year) is less aggressive than in chlorides (4.589 mm/year).
Corrosion rates (CR) of bare and coated alloys in NaCl – 55.47 wt.%KCl at 700°C in N2(g) atmosphere
192 µm/year (HVOF-NiCoCrAlY)
BSE-SEM image of HVOF–NiCoCrAlY (air, 900°C, 24 h, 0.5°C /min) after corrosion
(CR = 192 µm/year )
EDS [wt.%] | Phase |  | 
 | 12a | 12b | 12c
O | 22.8 | 31.2 | 20.2
Al | 0.3 | 2.2 | 26.1
Si | 0.8 | 1.0 | 1.2
Cr | 48.2 | 50.1 | 116.8
Fe | 1.1 | 1.2 | 0.6
Co | 5.5 | 2.3 | 12.5
Ni | 10.8 | 2.7 | 20.6
Y | 8.6 | 7.1 | 0.5

## Slide 8: Alumina Forming Alloys (AFA)
In702 (1050°C, 4h)
APMT (950°C, 8h)
HR224 (1050°C, 4h)
FESEM-EDS of pre-oxidized AFA alloys in zero air (ZA)
Mass and thickness losses of pre-oxidized alloys exposed to eutectic MgCl2 – 64.41 wt.% KCl at 700°C in flowing Argon up to 500 hours

## Slide 9: Corrosion of AFAs with Thermal Cycling
Corrosion rates of pre-oxidized alloys exposed to eutectic MgCl2 – KCl thermally cycled (700–550°C) under flowing Argon up to 175 hours
FESEM/EDS analyzes showed that oxide scales were not protective.
Cr-depletion was observed near the surface.
Alumina layers did not remain stable.

## Slide 10: AFA exposed to Molten Chlorides in an Oxidizing Atmosphere
Oxidizing atmospheres could be allowed if molten chlorides are exposed to pre-oxidized AFA alloys because alumina scales remained stable which did not occur in Ar atmospheres.
Long-term weight change corrosion tests will be required to determine corrosion rates and change of corrosion mechanism with time.
In702 (ZA, 1050°C, 4h) exposed to MgCl2 – KCl thermally cycled (550 – 700°C) under static ZA during 185 h.
Alumina remained stable and grew from ~5 to ~13 µm. There is no sign of localized intergranular corrosion.

## Slide 11: Supercritical CO2 Testing Facilities University of Wisconsin - Madison
Four systems with five total autoclaves
Temperature control allows system to operate within ± 1ºC
Testing temperature up to 750ºC for IN625 autoclave
Pressures up to 3600 ± 2 psi for IN625 autoclave
System operates at an average flow rate range of ~0.1 kg/h
  CO2 refresh rate ~ 2 h
Key Features
Mass spectrometer used for impurities other than O2/CO
  LLD: 10 ppm
  Accuracy: ± 5 ppm
Oxygen Sensor to measures concentration of O2 in CO2 bulk gas
  Accuracy: ± 1 ppm
Gas Chromatograph for low levels of CO in CO2 bulk gas
  LLD: 50 ppb
  Accuracy: ± 2.5 ppb

## Slide 12
Based on power fit equation:
Used time dependent data out to 1000 hours
Used ratio of thickness to weight change from SEM to determine approximate thickness of oxide after 1 year
The presence of C suggests that adding O2 does not completely stop the deposition of C during the oxidation.
Increase in Cr along grain boundary suggests presence of Cr-carbide.
Also resolved : i) void formation and Cr-depletion, ii) formation of Cr, and Fe-rich oxides, and iii) Al increase beneath oxide.
750ºC, 100ppm 750ºC, RG
H230 Cross-sections after 1000 h of exposure
EDS cross-sections of H230 after 1000 h of exposure in O2-doped CO2
Oxygen levels were recorded in CO2 gas before entering the testing autoclave (inlet), as well as at the exit of the autoclave for 650 and 750ºC tests. (Plotted for 100ppm test above)
Sample exposed to RG-CO2 showed no observable Cr-depletion zone.
Cr-depletion zone for O2-doped exposure in red box on right.
Cr-carbides found in both samples (indicated by red boxes on left side of both line scans).
sCO2 Corrosion Results

## Slide 13: Future of Corrosion Mitigation Approaches
Kinetic and corrosion mechanisms must be studied under higher oxidation potentials to determine if the AFAs can be used in chloride molten salts since it seems alumina protective layers are stable and could re-heal.
Vapor phase with oxidizing atmospheres are very aggressive to chromia forming alloys.
Samples exposed to CO2 without O2-doping produced less than 5 µm/year of extrapolated oxide. Significantly thicker oxides with evidence of spallation was obtained in O2-doped CO2. Adding O2 does not completely stop the deposition of C during the oxidation process. Carburization of the alloys exposed to sCO2 must be evaluated.