## Slide 1
Cermets for Energy Technologies
Edgar Lara-Curzio1, Bruce A. Pint1, Dongwon Shin1
Omer Dogan2, Darren Mollot3
  Oak Ridge National Laboratory
  National Energy Technology Laboratory
  U.S. Department of Energy –Fossil Energy Program Office
Collaborations with Ken Sandhage (Purdue University)
Innovation Forum
Washington DC.
November 15, 2018

## Slide 2
Outline
Background
Challenges and Opportunities
Selecting Materials for Applications
Composites and Cermets
W-ZrC Composites for sCO2 heat exchangers
Computational Materials Science & Engineering
Ongoing and Future Work (environmental stability and advanced manufacturing)

## Slide 3
1 Quad = 1x1015 BTU = 1.05 x1018 Joules
Estimated U.S. Energy Consumption (2017): 97.7 Quads = 102.6 EJ
Solar: 0.775
Nuclear: 8.42
Hydro: 2.77
Wind: 2.35
Geo: 0.21
Natural
Gas:
28.0
Coal:
14.0
Bio: 4.91
Electricity
Generation
37.2
12.5
Res.
10.7
Comm.
8.99
Industrial
25.2
Trans-
portation
28.1
Rejected
Energy
66.7
Energy Services
31.1
Petroleum:
36.2

## Slide 4
Direct-Fired
Indirect-Fired
sCO2 Power Cycles for Fossil Fuels
https://energy.gov/under-secretary-science-and-energy/sco2-power-cycles-fossil-fuels
sCO2 Power Cycles

## Slide 5
Subbaraman, Kung, and Saari (2018)
Materials in CO2 Environments

## Slide 6
Venus
The atmosphere of Venus is composed primarily of CO2.
The temperature on the surface is 740 K (467 °C, 872 °F), and the pressure is 93 bar (9.3 MPa)

## Slide 7
Subbaraman, Kung, and Saari (2018)

## Slide 8
Melting Temperature (°C)
Ni: 1455°C
Fe: 1538°C

## Slide 9
Highest Known Melting Temperature

## Slide 11
YOUNG’S MODULUS, E (GPa)
1000
100
10
1
0.1
0.01
CERMETS
W
Mo
WC
SiC
W-ZrC
M. F. Ashby, Materials Selection in Mechanical Design, Pergamon Press (1992)

## Slide 12
FRACTURE TOUGHNESS KIC (MPa m1/2)
1000
100
10
1
0.1
0.01
WC-Co
W
SiC
W-ZrC
M. F. Ashby, Materials Selection in Mechanical Design, Pergamon Press (1992)

## Slide 13
THERMAL CONDUCTIVITY (W/mK)
1000
100
10
1
0.1
0.01
W
W-ZrC
M. F. Ashby, Materials Selection in Mechanical Design, Pergamon Press (1992)

## Slide 14
STRENGTH AT TEMPERATURE (MPa)
10,000
1,000
100
10
1.0
0.1
W-ZrC
200
SiC
Ni ALLOYS
M. F. Ashby, Materials Selection in Mechanical Design, Pergamon Press (1992)

## Slide 16
Composite Materials

## Slide 17
Metal
Matrix
Composites
Cermets
Nomenclature
Randall M. German Particulate Composites: Fundamentals and Applications (2016)
Al-SiC
WC-Co
Ni-Ni3Al
50 nm
NbC
Stainless Steel
Precipitation-strengthened alloys

## Slide 18
Randall M. German Particulate Composites: Fundamentals and Applications (2016)
Composites

## Slide 19
Randall M. German Particulate Composites: Fundamentals and Applications (2016)
Composites

## Slide 20
Cermets are not new!
1925

## Slide 21
Cermets are not new!
1954

## Slide 23
Randall M. German Particulate Composites: Fundamentals and Applications (2016)
Cermets are widely used for
machining and cutting applications
WC-Co

## Slide 25
Thermodynamics
Tm=3,422°C
Tm=3,532°C
What temperature would be needed
to fabricate W—ZrC composites?
1,000°C

## Slide 26
½ Zr2Cu(l)+WC(s) → ZrC(s)+W(s)+ ½ Cu(l)
Thermodynamics
Displacement Reaction: Important Innovation!

## Slide 27
Thermodynamics
CuZr2

## Slide 28
https://www.energy.gov/sites/prod/files/2016/08/f33/PCHE%2006%20-%20Sandhage%20Purdue%20DE-EE0007117%20CSP%20Program%20Summit.pdf

## Slide 29
https://www.energy.gov/sites/prod/files/2016/08/f33/PCHE%2006%20-%20Sandhage%20Purdue%20DE-EE0007117%20CSP%20Program%20Summit.pdf

## Slide 30
https://www.energy.gov/sites/prod/files/2016/08/f33/PCHE%2006%20-%20Sandhage%20Purdue%20DE-EE0007117%20CSP%20Program%20Summit.pdf

## Slide 31
https://www.energy.gov/sites/prod/files/2016/08/f33/PCHE%2006%20-%20Sandhage%20Purdue%20DE-EE0007117%20CSP%20Program%20Summit.pdf

## Slide 32
W-ZrC Composite
Composition
58.1 ± 0.7 vol% ZrC
35.7 ± 0.4 vol% W
2.2 ± 0.6 vol% WC
4.0 ± 0.7 vol% Cu
ρ = 11.15 ± 0.03 g cm−3
porosity <3.0%
k = 66.0 ± 4.6 W m−1K−1
  2.5 to 3 times greater than that of Fe-based or Ni-based alloys
Flexural Strength
348 ± 45 MPa (20°C)
369 ± 22 MPa (800°C)
387 ± 14 MPa (800°C after thermal cycling)
Zr Map
W Map
W-ZrC — Caccia et al. (2018)

## Slide 33
W-ZrC — Song et al. (2002)
W-ZrC — Caccia et al. (2018)
Inconel 740 (Yield Strength) Guo et al. (2007)
Strength of W-ZrC

## Slide 34
W-ZrC Composite

## Slide 35
N. P. Padture, “Advanced structural ceramics in aerospace propulsion,” Nature Materials, vol. 15, August 2016
Thermal Conductivity (Wm-1K-1)
0
20
40
60
80
100
2,000
1,500
1,000
500
0
Temperature Capability (°C)
UHT
Carbides
UHT
Borides
W-ZrC
W-ZrC Composites Exhibit Outstanding Properties for Thermal Management Applications at High Temperatures

## Slide 36
Unfortunately, despite their high temperature resistance, all refractory metals oxidize severely at relatively low temperatures and therefore require oxidation-resistant coatings for elevated-temperature use in oxidizing environments.

## Slide 37
Copper melts at 1085°C!!!
https://www.energy.gov/sites/prod/files/2016/08/f33/PCHE%2006%20-%20Sandhage%20Purdue%20DE-EE0007117%20CSP%20Program%20Summit.pdf

## Slide 38
Environmental Testing

## Slide 40
Computational Materials Science

## Slide 41
½ Zr2Cu(l)+WC(s) → ZrC(s)+W(s)+ ½ Cu(l)
½ X2Cu(l)+ZC(s) → XC(s)+Z(s)+ ½ Cu(l)
Are there similar routes to synthesizing other refractory metal composites reinforced with carbide phases?
We are carrying out high-throughput thermodynamic screening to identify X and Z using CALPHAD databases starting with
SGTE*-SSUB**
*Scientific Group Thermochemistry Europe, ** SGTE SUBstance Database
Displacement reaction at 1400°C

## Slide 42
1 H |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2 He
3 Li | 4 Be |  |  |  |  |  |  |  |  |  |  | 5 B | 6 C | 7 N | 8 O | 9 F | 10 Ne
11 Na | 12 Mg |  |  |  |  |  |  |  |  |  |  | 13 Al | 14 Si | 15 P | 16 S | 17 Cl | 18 Ar
19 K | 20 Ca | 21 Sc | 22 Ti | 23 V | 24 Cr | 25 Mn | 26 Fe | 27 Co | 28 Ni | 29 Cu | 30 Zn | 31 Ga | 32 Ge | 33 As | 34 Se | 35 Br | 36 Kr
37 Rb | 38 Sr | 39 Y | 40 Zr | 41 Nb | 42 Mo | 43 Tc | 44 Ru | 45 Rh | 46 Pd | 47 Ag | 48 Cd | 49 In | 50 Sn | 51 Sb | 52 Te | 53 I | 54 Xe
55 Cs | 56 Ba |  | 72 Hf | 73 Ta | 74 W | 75 Re | 76 Os | 77 Ir | 78 Pt | 79 Au | 80 Hg | 81 Tl | 82 Pb | 83 Bi | 84 Po | 85 At | 86 Rn
87 Fr | 88 Ra |  | 104 Rf | 105 Db | 106 Sg | 107 Bh | 108 Hs | 109 Mt | 110 Uun | 111 Uuu | 112 Uub |  | 114 Uuq |  | 116 Uuh |  | 
 |  |  | 57 La | 58 Ce | 59 Pr | 60 Nd | 61 Pm | 62 Sm | 63 Eu | 64 Gd | 65 Tb | 66 Dy | 67 Ho | 68 Er | 69 Tm | 70 Yb | 71 Lu
 |  |  | 89 Ac | 90 Th | 91 Pa | 92 U | 93 Np | 94 Pu | 95 Am | 96 Cm | 97 Bk | 98 Cf | 99 Es | 100 Fm | 101 Md | 102 No | 103 Lr
X : 39 Elements
Z : 8 Elements (Ti, V, Zr, Nb, Mo, Hf, Ta, and W)
½ X2Cu(l)+ZC(s) → XC(s)+Z(s)+ ½ Cu(l)
Lara-Curzio et al. Cermets for Energy Technologies November (2018)

## Slide 43
Silica formers?

## Slide 44
Advanced Manufacturing: Binder Jetting
https://www.pinterest.com/pin/391602130070542236/

## Slide 45
Advanced Manufacturing: Binder Jetting + Melt Infiltration
ORNL. ARPA-E INTEGRATE (2018)

## Slide 46
Summary
ORNL, NETL, the U.S. Department of Energy –Fossil Energy Program Office and Purdue University are collaborating to develop high-temperature heat exchangers for sCO2 power cycles.
Current focus is on refractory metal matrix composites. Computational materials science tools are being used to identify candidate material systems.
Strategies are also being developed for providing environmental stability in sCO2 environments.
The feasibility of using advanced manufacturing (e.g., additive manufacturing) will be investigated to fabricate objects with complex shapes and to minimize energy intensity.