## Slide 1: High Performance, High Temperature Materials for High Efficiency Power CPS # 34924 Oak Ridge National Laboratory/Argonne National Laboratory/Siemens Corp. July 1, 2019–June 30, 2022
B. Pint, Oak Ridge National Laboratory
U.S. DOE Advanced Manufacturing Office Virtual Program Review
June 2-3, 2020
This presentation does not contain any proprietary, confidential, or otherwise restricted information.

## Slide 2: Overview
Timeline:
Project Start Date: 07/01/2019
Budget Period End Date: 03/31/2020
Project End Date: 06/30/2022
Budget | DOE Share | Cost Share | Total | Cost Share %
Overall Budget | $2,060,000 | $0 | $2.060.000 | 0%
Approved Budget (BP-1&2) | $2,060,000 | $0 | $2,060,000 | 0%
Costs as of 3/31/19 | $555,356 | $1,200 | $556,556 | 0.2%
Project Budget and Costs:
Barriers and Challenges:
Developing materials for ≥100°C increased temperature operation
Validating a component lifetime model using field exposed specimens
Identifying hot corrosion coating solutions with good mechanical properties for better fuel flexibility
Project Team and Roles:
ORNL: Technical lead on 3 tasks
ANL: advanced characterization
Capstone Turbine Corp: 65kW turbine operation and durability testing
Solar Turbines: field-exposed specimens
Siemens Corp: provide coatings for testing; feedback on test conditions and modeling
Tennessee Technological University: fabricate coatings for hot corrosion testing
AMO MYPP Connection:
CHP Materials challenges: lack of economical materials that can operate at higher temperatures and resist corrosion
Cost and complexity of installation and operation.
Reliability, availability, maintainability, and durability
Scalability: higher-efficiency 1-5 MW systems
Fuel flexibility: including renewable fuels
Project Title:
High Performance, High Temperature Materials for High Efficiency Power

## Slide 3: Project Objective(s)
(High Performance, High Temperature Materials for High Efficiency Power)
Develop higher performance and lower-cost materials to increase combined heat & power (CHP) system efficiency
Higher temperatures are needed to improve system efficiency
Innovative, high-temperature materials often are significantly more expensive or less reliable than current materials for 25-40 kh lifetimes
Objective: Develop materials solutions for ≥100°C using lifetime modeling validated by laboratory experiments and field exposures in conjunction with industry partners
  Approach: Identify materials solutions using laboratory experiments, field exposures, advanced characterization and validated lifetime models
    Industrial partners provided feedback and field exposed components
  Target: ≥100°C temperature increase
  Evaluating alumina-forming austenitic steels and hot c0rrosion coatings with appropriate fatigue resistance

## Slide 4: Technical Innovation
(High Performance, High Temperature Materials for High Efficiency Power)
Identifying high performance materials with reasonable cost to enable higher efficiency CHP systems
  Alumina-forming austenitic steels can achieve strength and oxidation resistance comparable to
Higher temperatures are needed to improve system efficiency
Innovative, high-temperature materials often are significantly more expensive or less reliable than current materials for 25-40 kh lifetimes
Objective: Develop materials solutions for ≥100°C using lifetime modeling validated by laboratory experiments and field exposures in conjunction with industry partners
  Approach: Identify materials solutions using laboratory experiments, field exposures, advanced characterization and validated lifetime models
    Industrial partners provided feedback and field exposed components
    Target: ≥100°C temperature increase
    Evaluating alumina-forming austenitic steels and hot c0rrosion coatings with appropriate fatigue resistance

## Slide 5: Technical Approach
Excellent industry team feedback on experiment parameters and critical materials issues
Evaluating new materials in laboratory testing
  ORNL Alumina-forming austenitic steel (Fe-base)
    850°C maximum temperature (Task 1)
  Newly patented Ni-base alumina-forming alloy
    1150°C maximum temperature (Task 2)
  Candidates coatings from industry
    700°C hot corrosion and fatigue testing (Task 3)
Modeling (Tasks 1 and 2)
Challenges
  Material available from industry partners or made at ORNL
  Choosing correct experiment parameters: industry feedback
  SO2 requires additional safety reviews
(High Performance, High Temperature Materials for High Efficiency Power)

## Slide 6
Technical Approach
(High Performance, High Temperature Materials for High Efficiency Power)
Modeling approach:
Parameters: %H2O, gas velocity, duty cycle, wall thickness…
Failure criteria:
  Using drop to 10%Cr at surface for initial predictions
  Observations from field exposed material may alter that metric
Oxidation lifetime diagram
Predict oxidation kinetics
Predict compositional changes (Cr-depletion)
800°C, 10,000h, 0.1 mm foil
800°C, 0.1mm foil
Dry air
Air + 10 % H2O
Measured
Calculated

## Slide 7: Results and Accomplishments (1 slide max)
(High Performance, High Temperature Materials for High Efficiency Power)
Milestone/Tasks | Status
Milestone 1.1 (Y1/Q1, FY19/Q4): Begin testing of new model alloys with different Mn levels | Achieved
Milestone 1.2 (Y1/Q2): Quantify alloy foil reaction rates after 1,000 h at 850°C | Achieved
Milestone 1.3 (Y1/Q3): Identify 2 corrosion coatings for fatigue testing | In Progress
Smart Milestone 1.4 (Y2/Q4, FY20/Q3): Evaluate 3 candidates based on 5,000 h 850°C exposures | In Progress
Milestone 2.1 (Y2/Q1): Initiate creep testing on new foil alloys | Achieved
Milestone 2.2 (Y2/Q2): Complete at least 3 fatigue experiments in SO2 | In Progress
Milestone 2.3 (Y2/Q3): Submit journal paper on lifetime modeling | In Progress
Smart Milestone 2.4 (Y2/Q4): Evaluate ≥2 coatings in corrosion and fatigue | In Progress
Go-No Go Decision (Y2/Q4): Identify 1 coating with adequate corrosion & fatigue | In Progress
Milestone 3.1 (Y3/Q1): Quantify precipitates in new alloy at ANL | In Progress
Milestone 3.2 (Y3/Q2): Submit journal paper on coating fatigue behavior | In Progress
Milestone 3.3 (Y3/Q3): Validate lifetime model | In Progress
Smart Milestone 3.4 (Y3/Q4): Using model, predict behavior within ±1s of experiments | In Progress
AFA steel has performed well after >2,000 hr at 850°C in laboratory testing in simulated exhaust gas (air + 10%H2O)
New equipment under construction for conducting fatigue testing under hot corrosion conditions (SO2 containing gas)

## Slide 8: Results and Accomplishments (1 slide max)
(High Performance, High Temperature Materials for High Efficiency Power)
Material received from industrial partners:
  Solar Turbines: provided foils exposed 106,000 hr in Mercury 50 duct
  Capstone: removed rainbow recuperator after 15,000 hr operation
  Siemens: coatings for hot corrosion testing
AFA steel has performed well after >2,000 hr at 850°C in laboratory testing in simulated exhaust gas (air + 10%H2O)
Initial results show promising results for two hot corrosion-resistant coatings
New equipment under construction for conducting fatigue testing under hot corrosion conditions (SO2 containing gas)
Modeling simulations initiated using advanced physics-based models and High-Performance Computing infrastructure (> 200 computational cores) to allow rapid predictions of material behavior during exposures in air + 10%H2O for up to 100kh as a function of time, temperature, alloy composition and gas flow rate.

## Slide 9: Transition
(High Performance, High Temperature Materials for High Efficiency Power)
First patent awarded for Ni-based alumina-forming alloy for 1150°C application in January 2019
Office actions are being pursued for a second patent on this class of alloys
Engaging with industry to increase TRL level to 4-5 for new Ni-based alloys and Fe-based AFA alloys
  Discussions with alloy manufacturers and end users
  Fabricating larger heats of new alloys