## Slide 1: Sodium Ion Expansion Power Block for Distributed CSP
Shekar Balagopal, Program P.I. Ceramatec, Inc.
Prof. Shannon Yee, Co. P.I. Georgia Institute of Technology

## Slide 2: Program Objectives
Develop a modular heat engine power block with an estimated efficiency (ηte) of 51.3%.
Program Goals:
Integrate ion-conducting electrochemical conversion materials into a heat engine
Establish ceramic manufacturing techniques to achieve record low membrane thicknesses
Apply 3D porous electrodes to minimize over potential losses
Develop evaporation and drop-wise condensation to realize high thermal efficiencies
Develop thermal-electric conversion system with design, modeling, and component testing
Assemble and demonstrate a >50% heat-to-electric power efficient breadboard validation in using a ~70 We module, with design scalable to a 1 kWe

## Slide 3: A Single Stage Sodium Thermo-Electro-Chemical Converter (Na-TECC)
Thermodynamic operation of a single-stage device.
Sodium is in liquid state. Liquid sodium is heated in evaporator, vaporizes and travels to anode.
Oxidation occurs at anode, and pressure gradient between hot cold side drives cations through the solid-electrolyte.
Electrons travel through load where power is extracted, and recombines with sodium and converts to liquid at condenser with heat rejection.
Sodium is cooled and condenses evaporator using a wick. Loop is closed via a capillary wick returning liquid sodium to evaporator.
Process modeled thermodynamically as isothermal expansion.
Temperature entropy diagram represents the ideal reversible cycle for a single stage
Notes: To understand the operation of the device let us begin with point 1, where the sodium is in liquid state. The liquid sodium is heated as it enters the evaporator, where it is vaporized and then travels to the anode shown here. The Na-TECC uses a special solid electrolyte that only allows the passage of sodium cations. So oxidation occurs at the anode, and the pressure gradient between the hot side and the cold side drives the flow of cations through the electrolyte. Meanwhile, the electrons travel through the load where power is extracted, and they recombine with the sodium cations in the cathode. This process can be modeled thermodynamically as an isothermal expansion. The sodium is cooled and condensed, and then it is pumped back into the evaporator using a wick. The temperature entropy diagram shown here with these steps represents the ideal reversible cycle for a single stage.

## Slide 4: What are the Advantages of a Na-TECC?
High second law efficiency (>90% of the Carnot limit)
High specific power (up to 0.2 kW/kg)
Closed system operation with no moving parts
Scalable to multiple power levels (100 W -10 kW)
Amenable to cogeneration using rejected heat
Notes: So what are the advantages of the Na-TECC?
The Na-TECC has a number of unique characteristics. The most prominent one being the high second law efficiency of the cycle. We see from the graph that at all operation conditions, the fraction of Carnot efficiency is greater than 90%. So for example, using reservoir temperatures of 1100 K and 500 K, the potential overall efficiency is almost 50%. The Na-TECC also has a high specific power. This allows us to use a small amount of sodium in our device, which is advantageous given that sodium is highly reactive. The system also has no moving parts, which minimizing mechanical failures. It is also closed system, so we do not have to deal with external mass transfer. The Na-TECC is scalable to a range of power levels, and I will show that this depends on the electrolyte area. Finally with a heat rejection temperature of about 500K, the waste heat is of a high grade, enough to make the Na-TECC and excellent candidate for cogeneration applications

## Slide 5: Improving the Efficiency by Using Multiple-Stages
The efficiency of a multiple-stages engine is:
Thot
Tcold
The thermal stress across the BASE is reduced
  less crack propagation
  lower loss of NaO2
  improved lifetime
Improved thermal management
  Lower parasitic heat losses
The Regeneration and Reheating steps allow the engine to reach lower temperatures
Staging is beneficial for the Na-TECC:
Notes: To overcome these small efficiencies in the real devices, we have conceived the idea of using multiple stages for the cycle. Now, any thermodynamic cycle can be broken into multiple stages as shown here, and the total efficiency is some product of the individual efficiency of each stage, given by this formula. Staging is beneficial to the Na-TECC for at least three important reasons. The Na-TECC suffers from several deteriorating effects due to the large temperature gradient along the thin BASE. These include crack propagation in the electrolyte and loss of sodium oxide. Due to time constraints, I will not go into the many other deterioration mechanisms. Staging reduces this thermal gradient, and thus reduces the associated thermal stress. This improves the lifetime of the BASE. The staging can help us improve the thermal management, which I will explain in more detail later on. Finally, a cycle with stages can take advantage of regeneration and reheating, which I will explain in more detail in the next slide.

## Slide 6: Dual Stage Process
With regeneration, the dual stage is thermodynamically favorable
ηdual = 52.3%
With dual stage cycle, the first expansion reaches an intermediate pressure and heat is regenerated for the second expansion from the isobaric cooling.
We can extract additional power through a reheat step.
This allows us to go to a lower temperature than with the single stage, using the same heat input
Notes: Regeneration and reheating can improve the thermal efficiency of a single stage cycle, such as the one shown above. With a dual stage cycle shown here, the first expansion reaches an intermediate pressure. For the second expansion, we can regenerate heat from the isobaric cooling step and use it for a part of the second isothermal expansion. We can complete the expansion by using a reheat step. This allows us to go to a lower temperature than with the single stage, using the same heat input. If we assume 100% regeneration (which is not farfetched with certain device configurations), the dual stage performs slightly better than the single stage. However, while this efficiency enhancement is good, it is not the primary motivation for the improved performance with a dual stage.

## Slide 7: Voltage and Efficiency of a Single Stage Na-TECC
Thot = 1150 K
Tcold = 550 K
Vopen = 1.09
Cumulative Voltage Drop
Cumulative Efficiency Drop
The largest efficiency drop is caused by parasitic heat loss (~40%)
Notes: These graphs show some representative values for a single stage Na-TECC operating with these conditions (point to table). Note that each successive curve represents the cumulative affect of different losses to the voltage and the efficiency. The voltage begins with the maximum open circuit value (1.09 in this case) , and is reduced by the cathode kinetic losses, then by adding the concentration losses ( which together make up the overpotential), and then by resistive losses. The same trends occur for the efficiency. Note that there is an extra contribution, which is the parasitic heat losses. This heat loss completely dominates the efficiency for a single stage. Previous devices have had upwards of 40% losses of the heat input. You will notice that the true efficiency is in the twenties, far away from the > 40% predicted for these working temperatures. The question becomes, “how can we improve the efficiency of these devices?”

## Slide 8
Voltage and Efficiency of a Dual
Stage Na-TECC
Cumulative Voltage Drop
Cumulative Efficiency Drop
Thot = 1150 K
Tint = 800 K
Tcold = 462.5 K
Vopen = 1.173
The largest efficiency drops are now caused by concentration losses and Joule heating
Notes: By applying regeneration and reheat, we can see some representative values for the dual stage device. These graphs are for the dual stage at these temperatures, the same ones used in the previous slide. As before, each successive line in the graph represents the cumulative contribution to voltage and efficiency. The largest efficiency drops come from the overpotential and the resistive losses. At this point, if you study the numbers you see that the dual stage actually performs worse than the single stage for the same rough values of temperature and other material properties when the heat loss is not accounted for. But why is this the case, when we showed improved performance before?

## Slide 9
Challenges
The dual stage has higher pressure losses, more Joule heating losses, and a larger overpotential than the single stage
The dual stage requires larger electrolyte area for the same power
However, the dual stage can have lower thermal losses than a single stage and thus better thermal management and higher efficiency
Challenges with the Dual Stage Operation
Temperature Profiles Illustration:
By adding a second stage, the hot and cold sides can be better thermally isolated from another
Single Stage
Dual Stage
Notes: Rather, the primary motivation is better thermal management because we are able to reduce the heat losses, given that the power generation is occurring in two stages each with smaller temperature differences.
The reason is that we have only looked at the ideal dual stage cycle. The issue with the dual stage is that it has higher pressure losses (with two expansion stages), more Joule heating losses (two sets of electrodes), and most importantly, higher overpotential losses from going to lower temperatures. Also, for the same electrode area the efficiency is much lower than the single stage due to the respective current density. Therefore, the main benefit of using dual stages is the improved thermal management, which ultimately leads to higher efficiency.
Consider the two schematics shown. These show the approximate temperature profiles and the approximate heat transfer direction. The second stage allows us to better shield the evaporator and condenser, and reduce heat losses (in particular the radiation loss). On top of these benefits, we have argued that the device lifetime can be dramatically increased with improved thermal management.

## Slide 10: Power Conversion
Beta-Alumina (Na2O-11Al2O3) is the Solid Electrolyte (BASE)
Mobile cation is sodium
Interstitial transport of cations through the conduction plane
Na+
Na+
e-
Na
1
2
3
4
Charge Transfer
Surface diffusion
Desorption
Diffusion
Anode
Cathode
Na+
Na+
e-
Na
Na+
Solid-Electrolyte
Notes: The solid electrolyte used by the Na-TECC is called beta alumina solid electrolyte, or BASE. The BASE is a compound of sodium oxide and alumina, and is combined with magnesium oxide to stabilize it. As shown in this drawing, the alumina components are arranged as slabs called spinel blocks. These are separated by thin regions containing the sodium oxide, called conduction slabs. The cations are transported along these conduction slabs through an interstitial transport mechanism. Basically, the conduction paths have vacancies and as the cations enter, they shift into these vacancies. These disturbances propagate along the path, pushing sodium out at the cathode. The ionic conductivity of the BASE is highly anisotropic; it is very high along the conduction path, and negligible in the orthogonal direction. The transport within the cathode itself is rather complex, but is essentially composed of four steps. Charge transfer at the phase boundary, surface to surface diffusion, desorption from the electrode surface, and finally diffusion to the condenser.

## Slide 11: Electrochemical Performance
Solid Na Ion conducing Electrolytes

## Slide 12: Key Project Milestones
Program 36 months: Budget: $2.34 M
Contract # DE-EE0007110

## Slide 13: Path to Market
This power block can be deployed for both:
  (i) small scale dish solar (displacing dish Stirling) and
  (ii) large scale heliostats and parabolic trough CSP.
Residential power modules is a high growth market to make high value electricity from consolidated solar energy at electricity cost
Target: 6 cents/kWhr depending on the region at an estimated cost of < $950 for kWe unit
Production sizes both
  (i) large volume production of several smaller distributed modules and
  (ii) a small number of large centralized power blocks can be realized with this technology

## Slide 14: Summary & Conclusions
Summary:
Discussed operation principles of dual stage Na-TECC
The cathode overpotential and concentration losses significantly reduce the voltage and efficiency
Introduced staging concept to improve efficiency
Conclusions:
Regeneration and Reheating can be used in a dual stage Na-TECC to improve the efficiency
Dual stage can ultimately achieve higher efficiency due to better thermal management and heat utilizations.
Acknowledgement:
Dr. Avi Shultz- Program Manager DOE-SunShot
Dr. Tom Hinklin, Marc Flinders, Joshua Johnston, Liz Smith
Dr. Andrey Gunawan, Alexander Limia, Jong Ha, John Kearns, Dr. Peter Kottke, Prof. Andrei Fedorov, and Prof. Seung Woo Lee
Notes: To recapitulate, we have discussed the operation of a single and dual stage, and how this technology works by using the special beta alumina solid electrolyte. We saw how the pressure losses and overpotential affect the voltage and the efficiency. And I introduced the cycle staging to improve the efficiency. In conclusion, regeneration and reheat improve the efficiency when employed in a dual cycle. The dual cycle, however, has higher parasitic losses. The dual cycle is ultimately beneficial because we are capable of better managing the heat transfer. We expect the dual cycle shown here, to perform better than typical single stage performance, shown here. Given this potential benefit, we believe the dual stage is worthy of further scientific inquiry.

## Slide 15: Sodium Ion Expansion Power Block for Distributed CSP
Shekar Balagopal, Program P.I. Ceramatec, Inc.
Dr. Shannon Yee, Co. P.I. Georgia Institute of Technology